# 6FM7(12V7.0Ah)

# The AILE sealed lead-acid rechargeable battery (SLA battery) is leak-proof and maintenance free. The Superiority of SLA battery is derived from its uniquely efficient oxygen recombination technology. The oxygen evolved from the positive plates diffuses through the microporous glass fiber mat to the negative plates where it is changed back to water by recombination reaction, eliminating the need for water addition .The result is a maintenance free battery.

Battery Construction

| Component | Positive plate | Negative plate | Container | Cover | Safety valve | Terminal | Separator | Electrolyte |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Raw material | Lead dioxide | Lead | ABS | ABS | Rubber | Copper | Fiberglass | Sulfuric acid |

| General Features | Application |
| --- | --- |
| ·Absorbent Glass Mat(AGM) technology for efficient gas recombination of up to 99% and freedom from electrolyte maintenance or water adding. ·Can be mounted in any orientation. ·Long service life , float or cyclic applications. ·Maintenance-free operation. ·Low self discharge. |  | ·Alarm System ·Medical Equipment ·Control Equipment ·UPS ·Communication Equipment ·Toys ·Emergency power System ·Power Tools |

# Specifications

| Nominal voltage | 12V |  | Capacity affected by temperature(20hr) | 40℃ | 102% |
| --- | --- | --- | --- | --- | --- |
| Capacity(20hr,25℃) | 7Ah |  |  | 25℃ | 100% |
| Design Life | 3-5 Years |  |  | 0℃ | 85% |
| Dimension | Length | 151mm(5.94inch) |  |  | -15℃ | 65% |
|  | Width | 65mm(2.56inch) |  | Self-discharge (25℃) | 3 month | Remaining capacity:91% |
|  | Height | 94mm(3.70inch) |  |  | 6 month | Remaining capacity:82% |
|  | Total height | 100mm(3.94inch) |  |  | 12 month | Remaining capacity:65% |
| Approx .weight | 2.32kg(5.11lbs) |  | Normal operating temperature | 25℃+3℃(77℉+5℉) |
| Capacity 77℉(25℃) | 20hr rate | 7Ah |  | Operating temperature range | -15℃~50℃(5~122℉) |
|  | 10hr rate | 6.51Ah |  | Float charging voltage(25℃) | 13.6 to13.8 V |
|  | 5hr rate | 5.95Ah |  | Cyclic charging voltage(25℃) | 14.5 to14.9 V |
|  | 1hr rate | 4.20Ah |  | Maximum charging current | 2.8A |
| Internal Resistance(Full charged Battery 77℉(25℃)) | 25mΩ |  | Terminal material | Copper |
|  |  |  | Maximum Discharge current | 105A(5 sec) |