短切毡：

定义：玻璃纤维短切原丝毡（简称短切毡）是将玻璃纤维经短切成50毫米长度后，无定向地均匀分布，经聚酯粉末、聚酯乳液粘结剂粘结而成的无碱或中碱玻璃纤维无纺毡制品。

Glassfibre chopped strand mat (briefly as CSM) is an non-woven E-or C-glassfiber glassfibre which is made of chopped strands of 50mm in length, which are randomly and uniformly dispersed and bound together with polyester binder in powder or emulsion form.

特点：

1.单位面积质量均匀，无污渍杂物等疵点， 
2.硬度适中，柔韧性好
3.易于完全浸透，制品气泡少，工艺性好。
4.具有很好的充模性和覆模性，适用于形状复杂的制品成型 
5.具有良好的机械力学性能和化学性能。

Product features

Uniform density, no any other impurity.

Proper rigidtitly, Excellent flexibility.

Good permeability easy for deaeration, good technics

Excellent processability in moulded parts, applying for diversity moulding and processing. Specially in opened moulding and closed moulding

Good mechanical physics and chemistry properties

产品包装，贮存与运输 packing storage and transport

短切毡应卷绕在内径为76mm的纸管上，每卷毡用聚乙烯塑料袋进行包扎，装入纸箱内。如短切毡宽幅为1040MM，外箱尺寸为：长28CM*宽28CM*高1070MM。产品垂直或水平放置。采用集装箱运输时可散装也可托盘包装。托盘包装时，每个托盘竖放16箱，托盘尺寸为：长112*宽112*高10CM。

短切毡贮存在干燥阴凉、防潮防雨的室内，建议温度控制在15℃～35℃，湿度控制在35%～６５％，如若不用请勿打开包装或扎紧包装口，以免受潮。

Products package and storage, transportation

Chopped strand mat will be wrapped up paper pipe of 76mm inner diameter, and polyvinyl chloride film will be used for packing and sealing and then package them with carton.such as width of 1040mm,The carton size will be:28L*28W*H1070cm the mats should be put horizontally or vertically. It’s allowed to be packaged by bulk and pallet when shipping by containers.When package by pallet ,each pallet vertially 16 cartons.The pallet size will be :112L*112W*H10 cm

Chopped strand mat should be reserved  indoor with drying, cool, wet-proof and rain-proof condition. It suggests that temperature should be control within 15℃～35℃ and humidity should be control within 35%～65%. The covering memberane shall be no opened until applying

应用：短切原丝毡主要应用于手糊成型，模压成型，离心浇铸成型,机械成型等玻璃钢成型缠绕工艺。可广泛应用于汽车附件，卫生洁具，化工防腐管道，冷却塔，贮罐、船舶、建筑构件,家具等各种玻璃钢制品。

The products are suitable for all kinds of FRP process, such as handing lay-up,

Filament winding, molding process. Centrifugally cast filled process. mechanical process,etc..It is widly used for automobile parts, sanitary wares, chemical corrosion resistance pipe, cooling tower, storage tank, ships manufacture, building materials, furniture and so on.

技术参数：technical parameter

| 性能 PROPERTY | 玻璃 类型 GLASS TYPE | 单位面积 质量 AREA WEIGHT g/m2 | 幅宽 WIDTH 200～3300 MM | 卷重 ROLL WEIGHT ㎏ | 含水率 MOISTURE CONTENT % | 可燃物含量 COMBUSTIBLE CONTENT % | 断裂强度 BREAKAGE STRENGTH N |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 测试方法 TEST METHOD | GB/T 1549 | ISO3374：2000 | ISO3374 | GB/T17470-1998 | ISO3344：1997 | ISO1887：1995 | ISO3342 |
| EMC80 | E/C-GLASS | 80±16 | ±5 | 6～95 | <0.2 | 13.6±0.35 | ≥200 |
| EMC100 | E/C-GLASS | 100±20 | ±5 | 6～95 | <0.2 | 9.5±0.35 | ≥170 |
| EMC150 | E/C-GLASS | 150±30 | ±5 | 6～95 | <0.2 | 8.0±0.35 | ≥40 |
| EMC225 | E/C-GLASS | 225±45 | ±5 | 6～95 | <0.2 | 5.0±0.35 | ≥60 |
| EMC300 | E/C-GLASS | 300±60 | ±5 | 6～95 | <0.2 | 4.0±0.35 | ≥90 |
| EMC450 | E/C-GLASS | 450±90 | ±5 | 6～95 | <0.2 | 3.8±0.35 | ≥120 |
| EMC600 | E/C-GLASS | 600±120 | ±5 | 6～95 | <0.2 | 3.6±0.35 | ≥150 |
| EMC900 | E/C-GLASS | 900±180 | ±5 | 6～95 | <0.2 | 3.4±0.35 | ≥180 |

无捻粗纱布（方格布）

定义：是由2000孔漏板拉制的直接无捻粗纱玻璃纤维按来纹组织编制而成一种片状双向增强织物.

Woven Rovings are bidirectional and enhanced fabric made by interweaving direct rovings which is leaked by 2000 hole board in plain weave pattern.

特点：

厚薄均匀、纤维排列密度大、无毛羽、污渍杂物

树脂浸透性好，脱泡性能好、施工率高。

经纬纱平行排列呈扁平状、张力均匀，很少扭转。

制品强度高、重量轻、耐腐蚀，使用寿命长。

Even thickness,good compaction of the fiber, no any other impurity and fluff

good permeability with resin easy for deaeration,high productivity

warp and weft rovings alignend in a parallel and flat manner resulting in uniform tension and very little twist.

High strength of the product, light weight, corrosion resistant,long time using.

应用：无捻粗纱布适用于各种树脂增强系统，广泛应用于手糊成型、模压成型和机械成型等玻璃钢成型产品，如船舶、容器、飞机和汽车部件、大型板材、家具、亚克力洁具、运动设施等领域。

Woven roving is in variety resin strengthen systems easy used for which is widely used in hands machanical process and paste the shaping crafts of glass fiber reinforced plastic.Such as shipping manufacture, vessles,planes and automotive parts, large panel, furniture, acrylic sanitary sports facilities and other fields.

包装:方格布卷在内径76mm或内径23mm的芯轴上，外套聚乙烯包装袋，装在瓦楞纸包装箱中

Roll Weight: 30-60kgs.Normal types are 36kgs.40kgs

Each roll Woven Rovings is would onto a paper tube,The mat roll is wrapped up with plastic bag,and then packed in a cardbard box or wrapped up with kraft paper.The rolls can be vertically or horizontally placed.For transportation ,the rolls can be loaded into a container directly or on pallets.

技术参数：

| 性能 PROPERTY | 单位面积 质量 AREA WEIGHT g/m2 | 纤维直径 FIBER DIA METER(μm) | 经纬纱WARP AND WEFT TEX | 经纬纱密度 WARP AND WEFT DENSITY root/inch |  |  | 织物密度 FABRIC DENSITY Root/cm |  |  | 含水率 MOISTURE CONTENT % | 可燃物含量 COMBUSTIBLE CONTENT % | 断裂强度 BREAKAGE STRENGTH N/50 (mm) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | WARP | WEFT |  | WARP | WEFT |  |  |  | WARP | WEFT |
| 测试方法 TEST METHOD | ISO3374：2000 | ISO1888:1996 | ISO3572:1976 | ISO4602: 1997 | ISO4602:1997 |  | ISO7211 -2:1984 | ISO7211 -2:1984 |  | ISO3344：1997 | ISO1887：1995 | ISO3342:2000 | ISO3342:2000 |
| EWR200 | 200±10 | 11 | 600 | 180 |  | 180 | 6.0 |  | 5.0 | ≤0.15 | 0.40-0.80 | 1300 | 1100 |
| EWR300 | 300±12 | 13 | 600/900 | 300 |  | 380 | 5.0 |  | 4.0 | ≤0.15 | 0.40-0.80 | 1800 | 1700 |
| EWR400 | 400±16 | 13 | 600/900 | 576 |  | 576 | 3.6 |  | 3.2 | ≤0.15 | 0.40-0.80 | 2500 | 2200 |
| EWR500 | 500±20 | 17 | 1200 | 900 |  | 900 | 2.9 |  | 2.7 | ≤0.15 | 0.40-0.80 | 3000 | 2750 |
| EWR600 | 600±24 | 17 | 1200/1200 | 1200 |  | 1200 | 2.6 |  | 2.5 | ≤0.15 | 0.40-0.80 | 4000 | 3850 |
| EWR800 | 800±32 | 24 | 2400/2400 | 2400 |  | 2400 | 1.8 |  | 1.8 | ≤0.15 | 0.40-0.80 | 4600 | 4400 |
| CWR200 | 200±10 | 11 | 600 | 180 |  | 180 | 6.0 |  | 5.0 | ≤0.15 | 0.40-0.80 | 1150 | 1000 |
| CWR300 | 300±12 | 13 | 600/900 | 300 |  | 380 | 5.0 |  | 4.0 | ≤0.15 | 0.40-0.80 | 1800 | 1600 |
| CWR400 | 400±16 | 13 | 600/900 | 480 |  | 500 | 4.0 |  | 3.8 | ≤0.15 | 0.40-0.80 | 2400 | 2200 |
| CWR600 | 600±24 | 17 | 200/1200 | 1300 |  | 960 | 2.6 |  | 2.6 | ≤0.15 | 0.40-0.80 | 3500 | 3000 |
| CWR800 | 800±32 | 24 | 2400/1750 | 2200 |  | 1760 | 2.0 |  | 2.0 | ≤0.15 | 0.40-0.80 | 4000 | 3600 |

缝编毡Stitch Mat

定义：玻璃纤维缝编毡（以下简称缝编毡），是由按一定方向排列的无捻粗纱或方格布作为基层材料，经短切成一定的长度后，无定向均匀平铺,用有机纤维缝编而成。

Fiberglass stitched mat is made from chopped fiberglass strands or woven roving which is cut into a certain length and randomly dispersed ,laid on a roving matrix then stitched together with organic fibers.

产品特点：

1. 均匀性好，湿拉强度高

2. 兼有机织布方向性及毡的多向性特点

3. 表面孔隙多，浸透好

4. 纤维结构具有可设计性

5. 不易产生位移变形，能保持最佳的力学性能

Even thickness, high wet tensile strength retention

Directional properties and strengths same to woven roving

Enough hollows on surface to make it good permeability

Flexibility to design variety weaving structures

Stable structure required to achieve maximum tensile strength properties

用途：
缝编毡应用于增强不饱和聚酯树脂并适用于拉挤成型、注射成型（RTM）、缠绕成型、手糊成型等玻璃钢成型工艺。如拉挤型材管道、贮罐、风力发电机叶片等制品。

Fiberglass stitched mat is used in unsaturated polyester resin strenthen, primarily in pultrusion, RTM, filament winding and hand lay-up processed. Such as pultruded parts, pipes, storage tanks, wind generator blades and other FRP products.

储存: 产品应堆放于干燥凉爽处，如若不用，请勿打开包装物或扎紧包装口，以免受潮。

stitch mat should be reserved indoor with drying, cool condition. It suggests that better to keep the package closed in order to prevent it from the wet.

包装: 缝编毡卷绕在内经为76mm的纸芯上，装入纸箱内.外套聚乙烯包装袋，袋口用聚酯绳采用活口扎紧，，然后码放在托盘上，每个托盘竖放12箱，横放9或6。托盘堆高不大于两层，纸箱堆高不大于三层。

Products package and storage, transportation

Stitch mat will be wrapped up paper pipe of 77mm inner diameter, and polyvinyl chloride film will be used for packing and sealing and then package them with carton.the mats should be put horizontally 12 and vertically 6 cartons every pallet.height of the pallet’s heap should be within the two layers of the pallet’s height.height of the carton heap should be within three layers of the carton.

技术指标Technical index

| 性能 property | 单位面积质量 Area weight | 玻璃类型 glass | 短切纤维/单重csm g/m2 | 粗纱或方格布/单重 twistless roving or woven roving g/m2 | 幅宽 width | 层数 layer | 含水率 moisture content | 可燃物含量combustible content % | 卷重roll/kg |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 测试方法 TEST METHOD | ISO3374 | GB/T 1549 | - | - | ISO5025 | - | ISO3344 | ISO1887 | - |
| CMK300 | -5±10 | C | 300 | - | ±3 | 单 | ≤0.3% | 6.9±1.4 | - |
| CMK380 | -5±10 | C | 380 | - | ±3 | 单 | ≤0.3% | 5.4±1.1 | - |
| CMK450 | -5±10 | C | 450 | - | ±3 | 单 | ≤0.3% | 4.5±0.9 | - |
| CMK580 | -5±10 | C | 870 | 870 | ±3 | 双 | ≤0.3% |  | 50 |
| EMK300 | -5±10 | E | 300 | - | ±3 | 单 | ≤0.2% | 6.9±1.4 | - |
| EMK380 | -5±10 | E | 380 | - | ±3 | 单 | ≤0.2% | 5.4±1.1 | - |
| EMK450 | -5±10 | E | 450 | - | ±3 | 单 | ≤0.2% | 4.5±0.9 | - |
| EMK580 | -5±10 | E | 870 | 580 | ±3 | 双 | ≤0.2% |  | 50 |

无捻粗纱

定义：无捻粗纱是玻璃钢基材的最基本形式，由多股平行的原丝拼合而成的粗纱（多股原丝无捻粗纱）或由一次拉制的多根单丝直接集束而成的粗纱(单股无捻粗纱).不同的无捻粗纱通过喷射、模压成型、缠绕等方式与聚酯或环氧树脂结合，形成高强度的玻璃刚制品。

Twistless roving is the fundamental mode of FGR.The twistless strand(Multi-fiber twistless roving) is pieced together from multiple parallel strand or from rhe multi-cluster strand which is put together directly by roving.The different kind of roving can be combined with polyester and epoxy through injection,molding,winding and so on,toform the FRP which has the FRP which has the high-strength.

1.拉挤纱 Pultrusion roving

特征：

硅烷型浸润剂处理
具有良好的耐磨性，毛丝少
纤维线密度稳定，具有高的单丝强度
可赋予复合材料高的物理化学性能、电气（绝缘）性能

Features：
good tensile force and excellent integrity
have excellent filament endurable for abrading and low fuzz
filament density steady, great filament tensile force 
easy wet out and impregnating and compatible with unsaturated polyester resin.

应用：

广泛应用于帐篷竿、玻璃钢门窗等产品。

Application:

Widely used for tent pole,FRP doors and windows etc.

包装：合股无捻粗纱，每个纱团用聚乙烯塑料袋进行包装，然后放入托盘或纸箱，每个托盘可码放48个或64个纱团，每个纱团重量17-20kg。可根据用户要求增加纱团重量。托盘堆高不大于2层，纸箱堆高不大于5层。

订货时请注明: ◎产品代号 ◎粗纱Tex值 ◎订货总重量 ◎包装方式 ◎如有特殊要求请注明

Package:
each direct roving roll covering by shrinkage membrane or drawing membrane, then placed into cardboard box or set on pallet. Each pallet can stack 48 or 64 rolls .each roll weight is 15-18kg. It is can increasing roll weight according to customer requirements. Pallet stack shall no be higher than 2 layers, cardboard box shall no be higher than 5 layers.

please remark followings in purchasing order: ◎ product code ◎roving TEX  ◎quantity ◎packaging requirement  ◎special needs can meet according to customer requirements.

贮存：产品应堆放于干燥凉爽处，如若不用，请勿打开包装物或扎紧包装口，以免受潮。

Storage:

Product shall be placed under dryness condition and shall no be open the covering membrane until applying.

技术参数：

| 产品代号 Product code | TEX | 单丝直径(um) Filament diameter | 适用树脂 Compatible resin | 适用工艺 Applying process | 烧失量% LOI |
| --- | --- | --- | --- | --- | --- |
| EPR | 1200-9600 | 11-13 | EP/UP | 拉挤、缠绕 filament winding, ultrusion, | 0.40-0.80 |
| EPR | 1200-9600 | 11-13 | EP/UP | 拉挤、缠绕 filament winding, Pultrusion, | 0.45-0.85 |

2．缠绕纱 Winding roving

特点：

硅烷型浸润剂处理
张力均匀，具有良好的成带性
具有良好的耐磨性，毛丝少
纤维线密度稳定，单丝强度高
与不饱和聚酯树脂有良好的相容性，快速、彻底的浸透

average filament tensile force and good integrity  have excellent filament endurable for abrading and low fuzz filament density steady and great filament tensile force easy wet out and high impregnating  endued good physical and chemical properties for final composite products.

应用:由“E”玻璃制成的连续纤维单股粗纱，适合于缠绕、挤拉成型工艺。
适用于不饱和聚酯树脂。

Applying for filament winding and pultrusion.
Compatible with epoxy resin, ethylene resin , and unsaturated polyester resin

包装：合股无捻粗纱，每个纱团用聚乙烯塑料袋进行包装，然后放入托盘或纸箱，每个托盘可码放48个或64个纱团，每个纱团重量17-20kg。可根据用户要求增加纱团重量。托盘堆高不大于2层，纸箱堆高不大于5层。

订货时请注明: ◎产品代号 ◎粗纱Tex值 ◎订货总重量 ◎包装方式 ◎如有特殊要求请注明

each direct roving roll covering by shrinkage membrane or drawing membrane, then placed into cardboard box or set on pallet. Each pallet can stack 48 or 64 rolls .each roll weight is 15-18kg. It is can increasing roll weight according to customer requirements. Pallet stack shall no be higher than 2 layers, cardboard box shall no be higher than 5 layers.

please remark followings in purchasing order: ◎ product code ◎roving TEX  ◎quantity ◎packaging requirement  ◎special needs can meet according to customer requirements.

贮存：产品应堆放于干燥凉爽处，如若不用，请勿打开包装物或扎紧包装口，以免受潮。

Product shall be placed under dryness condition and shall no be open the covering membrane until applying.

技术参数：

| 产品代号 Product code | TEX | 单丝直径(um) Filament diameter | 适用树脂 Compatible resin | 适用工艺 Applying process | 烧失量% LOI |
| --- | --- | --- | --- | --- | --- |
| EFW | 1200-9600 | 11-13 | EP/UP | 拉挤、缠绕﹑编织 filament winding,pultrusion, weaving | 0.40-0.80 |

3﹑喷射纱Spray up roving

特点:

树脂浸透性适中，与树脂有良好的相容性。

特别适用于喷射垂直面

贴膜性好，不回弹

易排气泡

切割性好

Proper  permeability of resin,have good compatibility of the resin.

Especially suitable for spraying up vertical plane.

Easy for sticking to the film.

Easy for deaeration

Easy for incising

应用：

主要用于制造玻璃钢船体，典型制品有座椅、水箱、汽车配件、卫生洁具、贮罐等玻璃钢制品

The products are suitable for all kinds of FRP hull.The tipical products  are seats，water tank,automobile parts, building materials, sanitary wares ，storage tank and so on.

包装：合股无捻粗纱，每个纱团用聚乙烯塑料袋进行包装，然后放入托盘或纸箱，每个托盘可码放48个或64个纱团，每个纱团重量17-20kg。可根据用户要求增加纱团重量。托盘堆高不大于2层，纸箱堆高不大于5层。

订货时请注明: ◎产品代号 ◎粗纱Tex值 ◎订货总重量 ◎包装方式 ◎如有特殊要求请注明

Each direct roving roll covering by shrinkage membrane or drawing membrane, then placed into cardboard box or set on pallet. Each pallet can stack 48 or 64 rolls .each roll weight is 15-18kg. It is can increasing roll weight according to customer requirements. Pallet stack shall no be higher than 2 layers, cardboard box shall no be higher than 5 layers.

please remark followings in  purchasing order: ◎ product code ◎roving TEX  ◎quantity ◎packaging requirement  ◎special needs can meet according to customer requirements.

贮存：产品应堆放于干燥凉爽处，如若不用，请勿打开包装物或扎紧包装口，以免受潮。

Product shall be placed under dryness condition and shall no be open the covering membrane until applying.

技术参数:Technical parameter

| 产品代号 Product code | TEX | 单丝直径(um) Filament diameter | 适用树脂 Compatible resin | 适用工艺 Applying process | 烧失量% LOI |
| --- | --- | --- | --- | --- | --- |
| ESR | 1200-9600 | 11-13 | UP,VE | 喷射，模压 Spray up roving,Moulding process | 0.40-0.80 |

4﹑制毡纱 Roving for chopped strand mat

特征：

硅烷型浸润剂处理
纤维线密度稳定，tex偏差小
低的静电积累，毛丝少
纤维硬挺度适中，具有优良的短切性，适合于动力分散
与饱和聚酯树脂有良好的相容性，具有高的透光度
可赋予复合材料高的物理化学性能

Product features：

Dealing with silane oftreating compound 
filament density steady and have excellent endurable of abrading .low fuzz
easy to chopping and good strands distribution.
soluble with UP resin, panel transparent light well.
endued good physical and chemical properties for final composite products

应用：

由“E”玻璃制成的连续纤维合股粗纱，适合生产制毡工艺
应用于增强不饱和聚酯树脂

Application

Applying for transparent panel process
Applying for reinforced UP resin.

包装：合股无捻粗纱，每个纱团用聚乙烯塑料袋进行包装，然后放入托盘或纸箱，每个托盘可码放48个或64个纱团，每个纱团重量17-20kg。可根据用户要求增加纱团重量。托盘堆高不大于2层，纸箱堆高不大于5层。

订货时请注明: ◎产品代号 ◎粗纱Tex值 ◎订货总重量 ◎包装方式 ◎如有特殊要求请注明

Packing    
Each direct roving roll covering by shrinkage membrane or drawing membrane, then placed into cardboard box or set on pallet. Each pallet can stack 48 or 64 rolls .each roll weight is 15-18kg. It is can increasing roll weight according to customer requirements. Pallet stack shall no be higher than 2 layers, cardboard box shall no be higher than 5 layers.

please remark followings in purchasing order: ◎ product code ◎roving TEX  ◎quantity ◎packaging requirement  ◎special needs can meet according to customer requirements.

贮存：产品应堆放于干燥凉爽处，如若不用，请勿打开包装物或扎紧包装口，以免受潮。

Storage
Product shall be placed under dryness condition and shall no be open the covering membrane until applying.

技术参数：Teachnical index

| 产品代号 Product code | 特克斯TEX | 单丝直径 Filament diameter（μm） | 适用树脂 Compatible resin | 适用工艺 Applying process | 烧失量 LOI% |
| --- | --- | --- | --- | --- | --- |
| ETR | 2400 | 11-13 | UP/EP | continuum process | 0.3-0.7 |
| CTR | 2400 | 11-13 | UP/EP | continuum process | 0.3-0.7 |

石膏纱：

石膏纱是通过硅烷偶联剂处理，专门用于增强石膏制品的一种玻璃纤维制品。

This gypsum roving is processed by silanre resin acceptor and specialized in fiberglass resinforced gypsum products

特点：

- 较好的短切性能，易于分散，无静电。

- 强度高、耐火、隔音、轻质。

- 硬挺度高，集束性好。

Products features

Good choppability,easy dispersion,no static.

Higher strength ,fire resistance,sound insulation and lighter in weight.

Good hardness,good beaming

应用

应用于建筑装潢等领域。石膏板、石膏装饰材料、雕塑。防火和各种装饰材料，如吊顶、隔板和隔音材料等。石膏线条。

Application

Widely used in building construction and decoration areas.

Gypsum plate,decorative material,sculpture

Fire resistance material and other decoration materials,such as suspended celling,clapboard and deadening,etc.

Gypsum ceiling

玻璃纤维薄毡 Glassfiber tissue

定义：Definition

玻璃纤维薄毡是由玻璃纤维原丝短切成的股纱，由造纸法随机均匀分布成连续玻璃纤维纸片，用乳剂粘结而成.

Glass fiber tissue is made of glass fiber yarn of 12mm in length, which made into sheet form by wet laid process.

特点：

1、浸渍性好，机械强度高、

2、耐化学腐蚀，绝缘

3、防火、阻燃、防水、防老化、耐气候性

High filter efficiency and mechanical strength
Chemical corrosion resistant and chemical insulation.
High fireproofing, fire retarding, water proof, aging resistant,weather fastness

分类：Types

玻璃纤维薄毡是采用德国湿法薄毡生产工艺，是良好的保温、消音、隔热、绝缘材料。根据其用途不同又分为玻纤屋面毡、玻纤地板毡、玻纤防水毡、玻纤短切毡等不同的型号。

Glass fiber mat is taking the method of the Dutch wet process mat which has good heat preservation, noisedamping, heat insulation and so on.It has wide range of applications depending on surface treatment method which is mainly used for reinforcing molded products in sheet form such as glassfiber roofing mat,glassfiber surface mat, flooring mat,water proofing mat , glassfiber chopped strand mat ,etc.

packing

包装: 薄毡卷绕在内经为76mm的纸芯上，装入纸箱内.外套聚乙烯包装袋，袋口用聚酯绳采用活口扎紧，，然后码放在托盘上，每个托盘竖放12箱，横放9或6。托盘堆高不大于两层，纸箱堆高不大于三层。

Products package and storage, transportation

Glassfiber tissue will be wrapped up paper pipe of 77mm inner diameter, and polyvinyl chloride film will be used for packing and sealing and then package them with carton.the mats should be put horizontally 12 and vertically 6 cartons every pallet.height of the pallet’s heap should be within the two layers of the pallet’s height.height of the carton heap should be within three layers of the carton.

屋面毡

定义：

屋面毡产品是制作SBS、APP改性沥青防水卷材和彩色沥青玻纤瓦的良好胎基，并且由于整幅毡的纵向加筋，充分提高了毡的纵向拉伸强度和抗撕裂强度。

Glassfiber roofing mat is the ideal substrate material for making SBS,APP  modification water proofing coiled  material and colorful bituminous glassfiber roofing tile. It enhanced the tensile strength MD and tearing strength for its whole tensile linear.

特点：

强度高，耐腐蚀性好 
尺寸稳定，沥青浸渍性好 
防脆裂、防老化、耐季候性强 
优良的防渗漏性

High strength and chemical corrosion

Stable size and good filter efficiency of the bituminous

Bursting preventing , aging resistant and weather fastness

Good permeability preventing.

应用：

玻璃钢制品、板材、管道、槽、罐、游船、浴盆等制品

环氧复铜板和电器绝缘制品

电池隔离片,屋面防水,石膏板护面板,塑料地板等防渗漏,防腐的优质材料

FRP, slab, pipeline,tanks,jags , boats and bath tubes products.

Composite copperplate and electricial insulating parts.

Battery separator,roofing for waterproof, gypsum wall board,synthetic resin floor, and other kinds of good quliaty material of leakage control and corrosion protection.

技术参数Technique index(fiberglass roofing mat)

| 型号 Type | 单位面积质量 Area weight | 加筋纱线密度 Linear density of reinforcement yarn | 筋纱间距Space Between Yarns | 纵向拉伸强度Tensile Strength MD | 横向拉伸强度Tensile Strength CMD | 水浸强度Wet MD Tensile Strength | 含胶率Binder content | 卷宽×卷长 Roll Width×Roll Length |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 单位 | g/m2 | tex | mm | n/5cm | N/5cm | N/5cm | % | mm |
| C-RTY45 | ±10% | 34-68 | 30 | ≥180 | ≥60 | 70 | 18 | 1000x3000 |
| C-RTY 50 | ±10% | 34-68 | 30 | ≥200 | ≥75 | 70 | 18 | 1000x2500 |
| C-RTY 60 | ±10% | 34-68 | 30 | ≥180 | ≥100 | 63 | 18 | 1000x2000 |
| C-RTY 90 | ±10% | 34-68 | 30 | ≥280 | ≥200 | 98 | 18 | 1000x1500 |
| C-RT 50 | ±10% |  |  | ≥170 | ≥100 | 60 | 18 | 1000x2500 |
| C-RT 60 | ±10% |  |  | ≥180 | ≥120 | 63 | 18 | 1000x2000 |
| C-RT 90 | ±10% |  |  | ≥280 | ≥200 | 98 | 18 | 1000x1500 |

玻璃纤维表面毡  Glassfiber surface mat

特征：

特有的生产工艺,决定其具有表面平整纤维分散均匀,手感柔顺,透气性好,树脂浸透速度快等特点

.表面毡产品适用于玻璃钢手糊成型，缠绕成型，拉挤型材，连续平板等工艺。

Product features

The glass mat for FRP surface has a fiber dispersion, smooth surface, soft hand-feeling, low binder content , fast resin impregnation and good mould obedience which make it most applicable to other FRP molding processes such as press moulding , spray-up, centrufugal rotating moulding.

技术参数 technique index(fiberglass surface mat)

| 型号 Type | 单位面积质量 Area weight | 纵向拉伸强度Tensile Strength MD | 渗透时间 Time of penatration | 含水率 | 卷宽×卷长/卷径/纸管内 Roll Width×Roll Length/diameter /paper core internal dia |
| --- | --- | --- | --- | --- | --- |
| 单位 | g/m2 | n/5cm | s | % | Mxm/cm/cm |
| C-RT20 | ±10% | ≥20 | ﹤8 | ﹤0.2 | 1.0x1000 ﹤100 15 |
| C-RT30 | ±10% | ≥25 | ﹤10 | ﹤0.2 | 1.0x1000 ﹤100 15 |
| C-RT50 | ±10% | ≥40 | ﹤16 | ﹤0.2 | 1.0x1000 ﹤100 15 |
| C-RT20 | ±10% | ≥20 | ﹤10 | ﹤0.2 | 1.0x1000 <100 15 |
| C-RT30 | ±10% | ≥25 | ﹤15 | ﹤0.2 | 1.0x1000 <100 15 |
| C-RT50 | ±10% | ≥30 | ﹤20 | ﹤0.2 | 1.0x1000 ﹤100 15 |

包装：

表面毡卷绕在纸芯上，外套聚乙烯包装袋，300米、卷包装时，一个20尺集装箱可以装273件

Products packing

The surface mat will be warpped up paper pipe,and polyvinyl chloride film will be used for packing.If packed into 300m per roll,one 20’ container will allow to 273 packages

连续石英玻璃纤维

　　一、技术规格： 　　
　　纤维细度：3～25μm 　　
　　纯　　度：SiO2含量99.9%以上 
　　二、性能： 　　
　　熔点：1710℃ 　　
　　析晶温度：700℃以上 　　
　　耐温性：1200℃半小时开始酥化不变型 　　
　　导热系数：（纤维毡状时）在200℃以下 < 0.03千卡/米·时·度 　　　　　　　　
　　在1000℃时0.2千卡/米·时·度 　　
　　抗拉能力：15.4N 　　
　　抗拉强度：常温下 > 150Kg/mm2 500℃时强度减少20% 　　
　　弹性模数：96×104Kg/mm2 　　
　　介电常数：ε=4.5 　　
　　体积电阻：（作电缆时） 　　　　　　　　
　　常温下>1×1017Ω·cm 　　　　　　　　
　　500℃时>1×1010Ω·cm 　　　　　　　　
　　1000℃时>1×108Ω·cm 　　
　　耐水性：在水中煮沸3小时无损失 　　
　　耐酸性：在1NH2SO4煮沸3小时无损失 　　
　　耐碱性：在0.5NNaOH煮沸3小时损失0.62% 
　　三、用途： 　　
　　①用于高温隔热：如火箭、导弹作隔热、防震材料或其它高温绝缘工程中。 　　
　　②用于增强塑料：与树脂合成制作高温高强度玻璃钢材料。广泛用于航空、导弹、火箭等方面。 
　　③特种电缆：做电缆的外包皮，用在高温特殊用途的电缆上。 　　
　　④用于高温酸碱过滤器。 　　
　　⑤用于电子管填充材料：水拉石英丝作为电子管的填充材料，以改善电子管的性能，延长电子管的寿命。

Continual quartz  glass  fiber

Teachnical  specialfections:

Fiber fineness: 3 ~ 25 μ m

Purity:more than 99.9 percent content of SiO2

Performance: Melting point: 1710 ℃

Crystallization temperature: 700℃ above

Thermotolerant  performance : 1200 ℃ half hour starts not to change form crisply.

Thermal coefficient: (mat-like) in the following 200 ℃ <0.03 kcal / m at the degree

In 1000 ℃ at 0.2 kcal / m at the degree

Tensile capacity: 15.4 N

Tensile strength: normal temperature  > 150Kg/mm2 500 ℃ at the strength reduced by 20%

Elastic modulus: 96 × 104Kg/mm2

Dielectric constant: ε = 4.5 
Volume Resistance: (for cable) 
At room temperature> 1 × 1017 Ω cm 
500 ℃ at > 1 × 1010 Ω cm 
1000 ℃ at > 1 × 108 Ω cm

Water tolerance: in the water boiled for three hours without loss

Acid resistance: 1 NH2SO4 boiled in three hours without loss

Alkaline resistance: 0.5 NNaOH boiled three hours loss of 0.62 percent

Applying:

- For high-temperature insulation: such as rockets, missiles for insulation, earthquake or other high-temperature insulating materials engineering.

- Used for reinforced plastic: high-temperature production of synthetic resin and high-strength glass fiber reinforced plastic materials. Widely used in aviation, missiles and rockets, and so on.

- Special cable: use for the foreskin of the cable, used in high temperature on the special-purpose cable.

- Acid-base for high-temperature filters

- For vacuum  tube  filled with  material: water Rafah as a quartz tube filled with silk material, in order to improve the performance of the tube,and extend the life of vacuum tube

玻璃纤维网格布定义玻璃纤维网格布是以玻璃纤维网布为基材，经表面涂覆作为定型耐碱处理而成的制品。  主要性能：强度高、耐碱、耐酸，与树脂粘性强，易溶于苯乙烯，硬挺性，定位性极强，是理想的增强材料。应用范围：水泥、塑料、沥青、大理石、屋面、墙面，马赛克，人造石，屋面防水及外墙外保温系统

湿法短切原丝（薄毡用纱）

1、定义：是由连续玻璃纤维原丝经短切成一定长度而制成，是制造玻璃纤维纸和薄毡的原材料。

2、应用：广泛应用于建筑材料，石油化学，照明工业，电器工业等。玻璃纤维纸和薄毡可以用作蓄电池的隔板、油毡。

3、特点：是易于水浆中快速均匀地分散。

4、包装：当25公斤/包时，一个20尺集装箱可以装16吨。

Fiberglass Wet Chopped Strand (roving for fiberglass tessue)

1、Definition

Wet chopped strand(roving for fiber glass tissue) are produced from continuous   filament strands and used as raw material of fiber

paper and fiberglass tissue mat.

2、Features

Wet chopped strands are featured by quick and easy dispersion in

pulp andslurry.

3、Applying

It is uses widely in building materials,petrochemistry,light industry

and electrical industry.etc.The main applications are battery separators,

asphalt felts,etc.